## Slide 1
The significance of ore mining districts
and associated metallurgical sites
Sandrine Baron
CNRS, TRACES laboratory, University of Toulouse, France
ERC SILVER Kick-Off Meeting, Lyon, France, January 21-24, 2018

## Slide 2
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 3
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 4
Metallurgical process
Lead bullion (Ag rich)
Slags
Litharge
Silver ingots
COINS and other precious materials
Cupellation
Merchant lead
Reduction
S. Baron
Galena ores
General principle of argentiferous lead chaîne opératoire
© Ch. Rico
Ore treatment structures (Cartagena, Spain)
Pb ingots (Saintes-Maries-de-la-Mer, France)

## Slide 5
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 6
Roman ingots versus Spanish ores
15 cm
Roman Lead Ingots
(Mediterranean wrecks)
Example : Trade of lead from Cartagena during Antiquity (Spain)
Trincherini et al., 2009
Comparison of isotopic signatures between ores and objects
Basque Ores
Almeria Ores
Cartagena Ores
Lead
ingots
Trincherini et al., 2009

## Slide 7
Example : Trade of lead from Cartagena during Antiquity (Spain)
Cartagena
    To trace the origin of the ores used for manufacturing the metal objects
    To point out the ancient metal trade routes
    (e.g. Budd et al., 1993 ; Stos-Gale et al., 1998 ; Niederschlag et al., 2003 ; Bode et al., 2009)
Comparison of isotopic signatures between ores and objects
Roman ingots versus Spanish ores
15 cm
Basque Ores
Almeria Ores
Cartagena Ores
Lead
ingots
Roman Lead Ingots
(Mediterranean wrecks)
Trincherini et al., 2009

## Slide 8
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 9
The mining districts themselves
The metallurgical processes : ores mixing, alloys elaboration, materials additions and recycling
    i.e Chaîne Opératoire
The available isotopic databases
Three main limiting factors
Notes: Four main factors limits the isotopic tracing : the ores geology though the isotopic signatures of the mining districts themselves (heterogeneity and / or similarities of different ores with different origin) and the lack of relevant ores databases. The second factor is the mixing ores, the alloys and the recycling. The third factor is analytical: the rise of accuracy and precisions of isotopic measurements allowing to more interpreted the data and to rise the isotopic differences. Les résultats d’analyses toujours plus pointues donnent des différences plus importantes car encore plus accentué entre les points analysés. Ce qui implique d’interpréter plus en profondeur ces différences et surtout pas de globaliser sans tenir compte de ces différences importantes. Autrement dit, la représentativité de l’échantillon est au coeur de la question. On ne doit pas analyser un échantillon qui ne représente pas assez la question posée et induira, de fait, des résultats non interprétables.
The fourthly factor is the metallurgical processes where several additions during the ores reduction could be realised … is the technical process operate to optimize the metal recovering.

## Slide 10
The mining districts themselves
The metallurgical processes : ores mixing, alloys elaboration, materials additions and recycling
    i.e Chaîne Opératoire
The available isotopic databases
The use of MC-ICP-MS which requires a relevant sampling
A last one…
Notes: Four main factors limits the isotopic tracing : the ores geology though the isotopic signatures of the mining districts themselves (heterogeneity and / or similarities of different ores with different origin) and the lack of relevant ores databases. The second factor is the mixing ores, the alloys and the recycling. The third factor is analytical: the rise of accuracy and precisions of isotopic measurements allowing to more interpreted the data and to rise the isotopic differences. Les résultats d’analyses toujours plus pointues donnent des différences plus importantes car encore plus accentué entre les points analysés. Ce qui implique d’interpréter plus en profondeur ces différences et surtout pas de globaliser sans tenir compte de ces différences importantes. Autrement dit, la représentativité de l’échantillon est au coeur de la question. On ne doit pas analyser un échantillon qui ne représente pas assez la question posée et induira, de fait, des résultats non interprétables.
The fourthly factor is the metallurgical processes where several additions during the ores reduction could be realised … is the technical process operate to optimize the metal recovering.

## Slide 11
Isotopic compositions
  => similarities between several mining districts through Mediterranean world and beyond
  => heterogeneities inside mining district and / or even inside a same lode
Ores selection
=> resources management linked with :
mining rights, coinage laws, ore content, geo political, economical stakes…
mining concessions, different owners (state, private…)
Ores sampling representativeness
        Difficult to recover precisely ore sources
Mining districts

## Slide 12
  Additions during chaîne opératoire due to the nature of the exploited ores
  => Optimize the precious metal recovering
  => Favour the slagging formation
Alloys
=> The whole of copper based materials
=> Coins : devaluation by metal additions
Recycling
=> Important for non ferrous metals
Metallurgical processes : possible disturbance of the tracer

## Slide 13
The available isotopic databases
Numerous lead isotopic databases exist (e.g. Oxalid)
To reject quickly some geographical areas
To propose some potential sources as metal origin but at too large scale
2. Nevertheless, the available databases have different granularity :
Some of them were established for geological case study
Others are coming from pedestrian prospecting without any archaeological context
Without multi isotopic measurements
Actually, it’s difficult to find THE mine(s) origin

## Slide 14
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 15
2. Mineralogy
ore deposition phases
nature of the exploited metal
specific minerals
3. Isotope Geochemistry
signature of a metal production
metallurgical processes understanding
new isotopic tracers development
Relevant Isotopic
Signature
1. Mining Archaeology
dated ores and slags
historical and cultural contexts
An interdisciplinary research at regional scale
Set up some isotopic databases which could be considered as referential
© C. Tamas
© B. Cauuet
Sn
Ag
Cu
Pb
Fe
…

## Slide 16
Example of using geological, chronological referenced materials
Baron et al., 2014
Refine the isotopic tracing
Understand the historical stakes
Exploited area =
Geo - Chrono referenced materials
Metallurgical wastes = Geo - Chrono referenced materials
Ores sampling during pedestrian prospections => NOT Geo-Chrono Referenced materials
Example: Silver Production, Medieval Times, South of France
=> Identification of lead signature of produced metal

## Slide 17
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 18
Archaeological examples
Iron mining district in Narbonne Province
Gold-Silver mining district in Roman Dacia
Gold-Silver mining district in Gaul

## Slide 19
    Iron metal production sites in South of France (1st c. BC to 2nd c. AD)
An iron waste structure in 1935
25 m high
=> 110 000 tons of produced iron for 300 years (Domergue Ed., 1993)
20 cm
The « Grand ferrier des Martys »
Excavations 1972-1978
Montagne Noire mining district

## Slide 20
Montagne Noire mining district hosted two kind of ores
100 μm
100 μm
    Iron metal production sites in South of France (1st c. BC to 2nd c. AD)
Gossan from primary sulfide ore
Gossan from primary carbonated ore

## Slide 21
Montagne Noire mining district hosted two kind of ores
Gossan from primary sulfide ore
100 μm
Gossan from primary
sulfide ores
Gossan from primary carbonated ores
Gossan from primary carbonated ore
100 μm
(Milot et al., 2016)
    Iron metal production sites in South of France (1st c. BC to 2nd c. AD)
=> Refining the traceability thanks to the use of ores exploited by ancient miners

## Slide 22
    Gold – silver production during Celtic period in France (6th to 3rd c. BC)
A minimum of 74 tons of produced gold
(Cauuet, 1999 ; 2005)

## Slide 23
    Gold – silver production during Celtic period in France (6th to 3rd c. BC)
(Baron et al., in prep)
Phase 1 : ores exploited by ancient miners (the richest ores in gold and silver)
Phase 2 : ores not exploited by ancient miners
=> narrow the isotopic signature of
production
(Cauuet, 2005)
(Cauuet, 2005)

## Slide 24
Trajan’s column, Rome
=> Praise of Dacia conquest
Dacia conquest was a real stake :
motivated by ores resources exploitation to hold the empire frontiers
Dacia conquest was decisive for roman economy i.e. 165 tons of gold and 331 tons of silver,
50 000 warriors, numerous gold and silver tableware…(Lydus, De Magistratibus, II, 28)
In 107 AD: apogee of Roman Empire
    Gold – silver production in Roman Dacia (1st to 2nd c. AD)

## Slide 25
    Rosia Montana mining district
© B. Cauuet
© B. Cauuet
- 6 Km long excavated galleries
- Discovering of numerous hydraulic systems
and ores treatment structures
Cauuet, 2012

## Slide 26
Gold Museum, Brad, Romania (4 cm long, photo G. Lehrberger)
Ores => Electrum, Ag > Au
0,1 mm
Baron et al., 2011
Cluj-Napoca
Bucharest
RM mining district
Baia Mare mining district
    Isotopic composition of Rosia Montana gold-silver ores

## Slide 27
(Backmann, 1995, Domergue 2008)
Ores do not contain enough Pb to set up a Au-Ag chaîne opératoire
    Gold – silver chaîne opératoire in Rosia Montana (1st to 2nd c. AD)
Lead additions => metal and/ or sulfosalts
=> Possible disturbance of the tracer

## Slide 28
Pb addition during the metallurgical process
    Gold – silver chaîne opératoire in Rosia Montana (1st to 2nd c. AD)

## Slide 29
Litharge trade is usual
Evidence in Spain
(e.g. Renzi et al., 2009 ; Murillo-Barroso et al., 2016)
Baron et al., 2011
In Rio Tinto mines (Spain), some Pb from Cartagena were imported to extract Ag from ores
=> Pb importation from other sources
    Gold – silver chaîne opératoire in Rosia Montana (1st to 2nd c. AD)

## Slide 30
The significance of ore mining districts
and associated metallurgical sites
General background
    Theoretical lead-silver chaîne opératoire
    Theory of metal provenance study
Limiting factors
Strategy
Archaeological examples
    Conclusion : expectations and required work for SILVER

## Slide 31
More generally, my expectations are
Estimate silver metal fluxes per mining district / mine(s) through history
Learn from others disciplines
Provide relevant referential to the community working on provenance studies
Re evaluate all ores databases by sorting them through geology, archaeological context and isotopic data (e.g. absence of 204Pb, presence of other isotopic measurements…)
Highlight mining regions underestimated as metal sources
Update the existing databases by acquisition of new samples and new isotopic data on unexplored or few documented mining districts / mines (Laurion…)
Investigate polymetallic ores treatments for silver production
Focus on ores and slags in archaeological context (acquisitions of samples from old excavations stored in museums or institutes and/or from excavations in progress…)
    My expectations for SILVER project

## Slide 32
Thank you for your attention
© Ch. Rico (Cartagena, Spain)